Sequences of operation

Fixed dentures:

Full crown

Made of metal alloy (gold or chromcobalt)

- Phase in dental office

Preparation –

Reduction 1 mm around, occlusaly 1, 5 mm

Preparation border. slight chamfer

Taking impression

Elastomeric impression materials

Polysulfid, silicon, elastomers.:

Retraction cord around the tooth

Dual viscosity technique or single viscosity technique.

Dual viscosity technique – double impression

Simultaneous dual viscosity technique

Antagonal impression

Alginate

Occlusal registration (wax, elastomeric materials)

- Phase in dental lab.

Making the cast (model) of gypsum.

There are three types of base raw materials derived from partial dehydratation of gypsum rock depending on on the nature:

Plasters – fluffy, porous, least dense.

Hydrocal – hihger density, more crystalline

Densite – densest of the raw material.

Plasters----- Model plaster, lab plaster

Hydrocal----dental stone

Densite ------High strength dental stone

High strength dental stone is used for fixed dentures.

Wax pattern

Lost wax method. – investment and casting, finishing.

- Phase in dental office

Try and cementation.

Sequences of operation

Fixed dentures:

Metal ceramic crown

Made of matal alloy ( usu chromcobalt) and ceramics which covers the metal framework

- Phase in dental office

Preparation –

Reduction 1 mm around, occlusaly 1, 5 mm

Preparation border. slight chamfer

Taking impression

Elastomeric impression materials

Polysulfid, silicon, elastomers.:

Retraction cord around the tooth

Dual viscosity technique or single viscosity technique.

Dual viscosity technique – double impression

Simultaneous dual viscosity technique

Antagonal impression

Alginate

Occlusal registration (wax, elastomeric materials)

- Phase in dental lab.

Making the cast (model) of gypsum.

There are three types of base raw materials derived from partial dehydratation of gypsum rock depending on on the nature:

Plasters – fluffy, porous, least dense.

Hydrocal – hihger density, more crystalline

Densite – densest of the raw material.

Plasters----- Model plaster, lab plaster

Hydrocal----dental stone

Densite ------High strength dental stone

High strength dental stone is used for fixed dentures.

Wax pattern

Lost wax method. – investment and casting, finishing of the framework

- Phase in dental office

Try  and colour choice

- making of ceramic

special procedure – firing in sesial oven in several phases.