## Slide 1: Restorative dentistry 3rd year Lecture 2
L. Roubalíková

## Slide 2: Composite materials
Chemically bonded mixture of organic
matrix and inorganic fillers

## Slide 3
Coupling agent – binds organic matrix and the filler together
Homogenous distribution of the filler particles in the material
Excellent mechanical properties

## Slide 4: Binding of the coupling agents to glass particles
CH2=C(CH3)-R
CH2=C(CH3)-R
CH2=C(CH3)-R
H O-Si
H O-Si
H O-Si
Double bond -polymerizable
Glass particle

## Slide 5: Importance of the components
matrix – a transfer mechanical loading on inorganic fillers, protects the filler against moisture
filler - a support of the material, carries the loading
coupling agents - a homogenous distribution of the filler in matrix

## Slide 6: Filler – material
Milled quartz
Aluminimum silicate glass
Silicium dioxide
Prepolymer (composite material is polymerized with high pressure in fabrics, than milled – particles of the fiiler are made of cured composite)
Complexes of microfiller (aglomerates) – e-g-. siliciumdioxide or zirconiumoxide

## Slide 7: Filler acc to the size of particles
Macrofiller ( size of particles µm ot tenth of µm )
Mikroplnivo (hundredths od µm)
Nanofiller (nm)
Combination– hybrid
Conventional (µm )
Microhybrid (hundredths od µm, µm)
Nanohybrid (hundredths od µm, µm, nm)

## Slide 8: Macrofiller
Particles µm or tenths of µm
Good mechanical resistance , abrasion resistance, bad polishability.

## Slide 9: Microfiller
• Silicium dioxide (pyrogenous)
• Particles hundreths µm
Less amount of filler due to big surface
Lower mechanical resistence, good polishability.

## Slide 10: Microfiller in complex particles
Prepolymer
Aglomerates
- Higher amount of filler, good mechanical resistance, good polishability

## Slide 11: Nanoparticles
Particles 10 nm and less
Special technology, size, shape and binding to monomer

## Slide 12: Today
Microhybrid or nanohybrid composites:
Good mechanical properties, good polishability, propagation of cracks is minimized.

## Slide 13: Matrix
Bis GMA – Bowen´s monomer • (2,2-bis[4-(2hydroxy-3-metakryloyloxypropoxy) • fenyl]propan)
• Bis DMA
• UDMA
• TEGMA /triethylenglykoldimethacrylate
• EGMA ethylenglykoldimethacrylate
• e Bis –GMA
• HDMA hexandioldimethacrylate
Dimethacrylates - mixture of materials with high and lower molecular weight

## Slide 14: Matrix - modification
- Acid modified resins (compomers)
Polysiloxan chains with
polymerizable groups (ormocers)
- Silorans (ring opening monomers)

## Slide 15: Coupling agent
G -methacryloxypropyltrimetoxysilan (A 174)

## Slide 16: Other components
Activator and initiator
Pigments
Fluorescents
Absorbers of light
Inhibitors

## Slide 17: Selfcuring composites
Activator Initiator
Dibenzolyperoxide Tertiary amine
Initiator Activator

## Slide 18: Light curing composites
Initiator and sometimes also activator
Camphorchinon CQ
Phenylpropandion PPP
Trimetylbenzoylphosphino xid TPO

## Slide 19: Camphorchinon (CQ) - initiator
Yellow colour
Activator is present: etyl-4-(N,N’-dimetylamino)benzoát (4EDMAB), N,N’-dimetylaminoetylmetakrylat (DMAEMA)
Light shades of composites: combination of CQ and other initiators.

## Slide 20: Composite materials – basic characteristics
Matrix Filler
Compressive strength
Elasticity
Polymerization shrinkage
Polymerization stress
Water sorption

## Slide 21
Classification of composite filling materials
Size of the filler particles
Macrofilled, microfilled (homogenous, non homogenous, hybrid)
Matrix (monomers)
Dimethacrylate, acid modifies, ormocers, silorans
Viskosity (flowable, thick)

## Slide 22: History
Dimetacrylates
Bowen 1960 – Bowen´s monomer
Buoconore 1955 – acid etching

## Slide 23: History
Fusayama 1979
Adhesion to dentin
Yoshida. Nakabaiashi
Van Meerbeck

## Slide 24: 35% - 37% phosphoric acid silica particles blue dye

## Slide 26: Adhesion
Mechanical adhesion
Specific adhesion
Intermolecular forces
Chemical binding

## Slide 27
Enamel

## Slide 28
Acid on aprismatic enamel
Acid on prismatic enamel

## Slide 29
Dentin
Bonding agent

## Slide 30: Adhesive system connects resin to enamel and dentin
Bond is a hydrophobic resin principally of the same composition as composite filling material but without the filler or with a small amount of filler. It works in enamel. In dentin primer is necessary before bond.
Why?

## Slide 31: Dentin – special composition
More water – always wett
Less minerals
Low surface energy
Smear layer
Composite is hydrophobic, we need hydrofilic substance

## Slide 32: Adhesive systems contain resin monomers
Hydrophobic monomers - bond works in enamel it does not work in dentin without primer
Amphiphilic monomers – hydrophobic + hydrophilic part - in primer
Primer is necesssary for dentin.
The hydrophillic part flows into dentin (tubules, spaces in collagen network) and keep the collagen network open, the hydrophobic part of primer binds to hydrophobic bond that flows into dentin pretreated with primer-
If primer applied on enamel – residual of water can be removed.

## Slide 33: Adhesive systems contain resin monomers Primer:
4-META •
HEMA •
TEGMA •
PENTA P •
5-NMSA •
Bis-GMA
Bond: Bis-GMA ot other dimetacrylates. Hydrophpobic.

## Slide 34: Dissolving agents
Aceton
Alcohol
Water
Water/alcohol

## Slide 36
Acid etching | Rinsing | Priming |  | Bonding
Acod etchin | Rinsing | Priming a bonding |  | 
Selfetching priming |  |  | Bonding | 
Selfetching bonding) |  |  |  | 
Clinically oriented classification of
the adhesive systems acc
to number of steps

## Slide 38: Srelfetching bonding agents

## Slide 39
TE – Total etch,
ERA
SE – Self etching
SEA

## Slide 40: Two steps selfetching agents
Acidic hydrophilic primer – evaporation of the solvant, penetration, dissolving of the smear layer
Hydrofobic bond – sealing of the surface

## Slide 41: One step selfetching agents
More vulnerable bonding, risk of hydrolysis
FAKT !!!

## Slide 42
Source: Dudek M. Adhezivní spoj
a adhezivní systémy I. LKS 11/2013
Smear layer layer
Dentin
tubules
pH of the adhesive system
thickness of the hybrid layer
surface of dentin smear layer impregnated resin tag
with the adhesive system
very mild acidic sea
mild acidic sea
acidic sea
strong acidic sea

## Slide 43
Colagen fibers with interfibrilar and
Instrafibrilar crystals od hydroxyapatite
Colagen fibers with intrafibrilas crystals
of hydrpoxyapatite only
Colagen fibers without crystals
of hydroxyapatites
Zdroj obrázku: Dudek M. Adhezivní spoj
a adhezivní systémy I. LKS 11/2013

## Slide 44: Importance of hydroxyapatite
Protection of collagen against hydrolysis
as well as enzymatic degradation of collagen (due to activation of matrix metaloproteinasis)
Strong mineral acid id dangereous for good long term bonding
Clorhexidin for one minute can stabilize collagen

## Slide 45
Enzymatic degradation of
collagen

## Slide 47: Factors affecting quality of bonding
Structure and composition of hard dental tissues
Quality of their surface – esp. presence of smear layer, contamination with moisture, saliva and blood
Configuration factor – C- factor
Mechanical loading of the adhesive connection
Oral environment and external chemical materials (tooth pastes, asntiseptics, bleaching agent rtc.)

## Slide 48
Monomer
Light
Polymerization
Polymer

## Slide 49
Pre –gel
Gel
Post -gel
Pre gel phase should be long – soft start !!!!

## Slide 50: Three phases
Phases
Pre-gel – material is soft
Gel-point – material became hard
Post –gel – material is not soft, postgel shrinkage

## Slide 51
Photocomposite
102mm
48mm

## Slide 52
Photocopomosite
3,2mm
57 mm
3mm
8,5mm

## Slide 53
Selfcuring composite
434343
43mm
42mm

## Slide 54: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 55: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 56
High content of filler increases the modulus of elasticity
High modulus of elasticity increases the polymerization stress
High content of filler decreases the polymerization shrinkage
Polym. Stress
Modulus of elasticity
Polymerization shrinkage

## Slide 57: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 59
5
2
1
Bonded area : Free area
1:1 and less - optimal

## Slide 60: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 61: Mode of application
Incremental technique
Layer by layer with big free surface
Importance of flowables
Thin layer of flowable first –big free surface
Good marginal adaptation
Compensation of the stress of the other layers
Bulk fill materials do not solve the problem with polymerization stress

## Slide 62
Placement of the material

## Slide 63: Placement of the material
Photocomposite
Thin layer with the maximal free surface (with respect of C-factor of each layer)
Combination of materials of various viscosity
GIC + photocomposit (two visits better)
Increment of cured material into the soft non
cured material

## Slide 64: Consequences of high C- factor
White line around the filling
Sealing of the filling . Acid etching around the cavosurface margin,
application of the unfilled resin

## Slide 65: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 66
Fotokompozit
102mm
48mm

## Slide 67
Selfcuring material
434343
43mm
42mm

## Slide 68: Duration of pre-gel phase
Longer pre-gel phase is better for releasing of polymerization stress
Soft start
Combination of materials (selfcuring composite materials have longer pre gel phase)

## Slide 69: Factor that influence the quality of bonding
Configuration factor – C- factor +polymerization stress
Structure and composition of hard dental tissues
Quality of their surface – esp. presence of smear layer, contamination with moisture, saliva and blood
Mechanical loading of the adhesive connection
Oral environment and external chemical materials (tooth pastes, asntiseptics, bleaching agent rtc.)

## Slide 70: Cpontemporary possibilities polymerization
Quarz halogen units (halogen lamp)
Plasma units
LED units (diode – monocgromatic light, need of more diods)
Laser (strictly monochromatic light)

## Slide 71: Polymerization units – output energy
Quarz halogen
LED (3.generation)
Plasma
600 -800 mW/cm2
1000 -1800 mW/cm2 modré
50 – 100 mW/cm2 fialové
1500 - 2000mW/cm2

## Slide 72: Output energy and time of polymerization
Recomended power is 12000 – 16000 mJ/cm2
12 000 mWs/cm2
measured intensity mW/cm2
Time in seconds
Usually 20 s
Radiometer ois recommended

## Slide 73: Photoinitiators
Kafrchinon
CQ
Phenylpropandion
PPP
Trimetylbenzoylphosphinoxid TPO

## Slide 74: Absorbtion spectrum of fotoiniciators
Photoinitiator | Absorbtion spectrum (nm) | Maximum (nm)
CQ | 440 - 500 | 470
PPD | 380 – 430 | 400
TPO | 350 - 410 | 380

## Slide 77: Light conductor
Small area – higher concentration of output energy, but bigger dispersion
The average distance is 4 mm – 10 mm.
Standard light conductor – more reliable for daily is
Standardní a kónický světlovod

## Slide 78: Mode of curing
Continuous curing at a constant intensity level: 40s of 500 mW/cm2
Continuous two step curing
10 s 150 W/cm2 then 750 mW/cm2
for remaining time
Two step ramp – low intensity level gradually increases (5-10s) to achieve a final high intensity
Puls delay
Low intensity short time, 100 - 300 mW/cm2unit is turn off. 3 min pause
Final curing 600 mW/cm2
Othe factors for consideration
Shade
Increments towards dentin walls
Pulse delay technique is dedicated to the layer that contacts enamel

## Slide 79: Flowables
– marginální adaptation (material flows)
- small polymerization stress – importance in incremental technique
- block out of undercuts
- small cavities, corrections

## Slide 80: Composite materials with high viscosity
Small polymerization shrinkage
Hihg polymerization stress
Worse marginal adaptation

## Slide 81: Bulk fill
Application and curing in one bulk
Higher amount of fotoinitiators
Higher translucency
The problem with polymerization stress is not comlpetely solved
Group of various materials:
Flowables
Condensables
Sonic Fill (KaVo)

## Slide 82: Sonic Fill
Big bulk up to 5mm (less – 4 mm
is recommended)
Sonic „activation“ – vibration
decrease viscosity
Internal dispersion of light
Long term expeerience?

## Slide 83: Factors that influence the quality of bonding
Structure and composition of hard dental tissues
Quality of their surface – esp. presence of smear layer, contamination with moisture, saliva and blood
Configuration factor – C- factor
Mechanical loading of the adhesive connection
Oral environment and external chemical materials (tooth pastes, asntiseptics, bleaching agent rtc.)

## Slide 84: Working procedure and variables affecting the bonding

## Slide 85
What affects the quality of bonding?

## Slide 86: Variables that affect quality of bonding
1) Etching
Etching too long can etch too deep, making it difficult for the resins to reach sound tooth structure.
1.9µm

## Slide 87: Variables that affect quality of bonding
2) Drying dentin
Over drying the dentin after etching can be very destructive to bond values with some adhesives.

## Slide 88: Variables that affect quality of bonding
3) Application time
Too short of application time may not allow for proper volatilization of the solvents or complete resin hybridization. This is critical with self etching systems.

## Slide 89: Variables that affect quality of bonding
4) Thinning / drying
Too thin of adhesive layer doesn’t allow for proper curing due to oxygen inhibition. Too thick and the adhesive may still contain solvents.
O2
O2
O2
O2
O2
O2

## Slide 90: Air thin / Dry
TO TRANSLUCENCY

## Slide 91: Variables that affect quality of bonding
5) Light curing
Too short or insufficient light cure equals partially polymerized resins.

## Slide 92: Variables that affect quality of bonding
6) Composite Placement
Improper adaptation of the composite to the adhesive can create voids at the bonding interface.
Condenser

## Slide 93: Variables that affect quality of bonding
7) Contamination
Blood
Sulcular fluid
Saliva
etc…

## Slide 94: Variables that affect quality of bonding
8) Deteriorated product
Expired
Volatilized

## Slide 96: Indication of composite materials
Filling of all classes:
I., II. class: small to moderate restorations
III. Class
IV. Class
V. Class
Other factors for consideration:
Level of oral hygiene
Occlusal loading
Quality of hard dental tissues

## Slide 97: Other indication
Splinting
Postendo treatment (post and core)
Cementation (special materials) – adhesive cementation
Fissure sealing
Venners – direct, indirect

## Slide 98: Contraindication of composite materials
Bad level of oral hygiene
Large cavities in posterior teeth (alternative is amalgam or inlay/onlay,
Heavy occlusal stress (deep bite , bruxis)
Cavities out of enamel (esp. cervical area)
Social aspects

## Slide 100: Postendo – post and core

## Slide 101: Postendo using flowable and onlay
Flowable at the bottom
Composite onlay
Onlay after 8 years

## Slide 108
lenka.roubalikova@tiscali.cz