## Slide 1: Restorative dentistry III.
Repetition

## Slide 2: Composite materials
Chemically bonded mixture of organic
matrix and inorganic fillers

## Slide 3
Coupling agent – binds organic matrix and the filler together
Homogenous distribution of the filler particles in the material
Excellent mechanical properties

## Slide 4: Binding of the coupling agents to glass particles
CH2=C(CH3)-R
CH2=C(CH3)-R
CH2=C(CH3)-R
H O-Si
H O-Si
H O-Si
Double bond -polymerizable
Glass particle

## Slide 5: Importance of the components
matrix – a transfer mechanical loading on inorganic fillers, protects the filler against moisture
filler - a support of the material, carries the loading
coupling agents - a homogenous distribution of the filler in matrix

## Slide 6: Kompozitní materiály podle plniva
Makroplnivo - makrofilní
Mikroplnivo – mikrofilní
Kombinace – hybridní
konvenční hybridní
mikrohybridní
Kompozity s nanoplnivem

## Slide 7: Composition - matrix
Bis GMA – Bowen´s monomer • (2,2-bis[4-(2hydroxy-3-metakryloyloxypropoxy) • fenyl]propan)
• Bis DMA
• UDMA
• TEGMA /triethylenglykoldimethacrylate
• EGMA ethylenglykoldimethacrylate
• eBis –GMA
• HDMA hexandioldimethacrylate
Dimethacrylates

## Slide 8: Composition – matrix
- Acid modified resins (compomers)
Polysiloxan chains with
polymerizable groups (ormocers)
- Silorans (ring opening monomers)

## Slide 9: Filler
Milled quartz
Aluminimum silicate glass
Silicium dioxide
Prepolymer
Complexes of microfiller (aglomerates)

## Slide 10: Macrofiller
Particles µm or tenths of µm
Good mechanical resistance , abrasion resistance, bad polishability.

## Slide 11: Microfiller
• Silicium dioxide (pyrogenous)
• Particles hundreths µm
Less amount of filler due to big surface
Lower mechanical resistence, good polishability.

## Slide 12: Microfiller in complex particles
Prepolymer
Aglomerates
- Higher amount of filler, good mechanical resistance, good polishability

## Slide 13: Nanoparticles
Particles 10 nm and less
Special technology, size, shape and binding to monomer

## Slide 14: Coupling agent
G -methacryloxypropyltrimetoxysilan (A 174)

## Slide 15: Other components
Activator and initiator
Pigments
Fluorescents
Absorbers of light
Inhibitors

## Slide 16: Selfcuring composites
Dibenzolyperoxide Tertiary amine
Initiator Activator

## Slide 17: Light curing composites
Initiator and sometimes also activator
Camphorchinon CQ
Phenylpropandion PPP
Trimetylbenzoylphosphino xid TPO

## Slide 18: Camphorchinon - CQ
Yellow colour
Activator: etyl-4-(N,N’-dimetylamino)benzoát (4EDMAB), N,N’-dimetylaminoetylmetakrylát (DMAEMA)
Light shades of composites: combination of CQ and other initiators.

## Slide 19: Composite materials – basic characteristics
Matrix Filler
Compressive strength
Elasticity
Polymerization shrinkage
Polymerization stress
Water sorption

## Slide 20
Classification of composite filling materials
Size of the filler particles
Macrofilled, microfilled (homogenous, non homogenous, hybrid)
Matrix (monomers)
Dimethacrylate, acid modifies, ormocers, silorans
Viskosity (flowable, thick)

## Slide 21: History
Dimetacrylates
Bowen 1960 – Bowen´s monomer
Buoconore 1955 – acid etching

## Slide 22: History
Fusayama 1979
Adhesion to dentin
Yoshida. Nakabaiashi
Van Meerbeck

## Slide 24: Adhesion
Mechanical adhesion
Specific adhesion
Intermolecular forces
Chemical binding

## Slide 25
Enamel

## Slide 26
Acid on aprismatic enamel
Acid on prismatic enamel

## Slide 27: Dentin – special composition
More water – always wett
Less minerals
Low surface energy
Smear layer
Composite is hydrophobic, we need hydrofilic substance

## Slide 28
Dentin
Bonding agent

## Slide 30: Adhesive systems contain resin monomers
4-META •
HEMA •
TEGMA •
PENTA P •
5-NMSA •
Bis-GMA

## Slide 31: Adhesive systems contain resin monomers
Hydrophobic monomers - bond Works in enamel Does not work in dentin without primer
• Amphiphilic monomers – hydrophobic + hydrophilic part - primer
Primer is necesssary for dentin. If applied on enamel – residual of water can be removed.
lroubalikova

## Slide 32: Dissolving agents
Aceton
Alcohol
Water
Water/alcohol

## Slide 33
Acid etching | Rinsing | Priming |  | Bonding
Acod etchin | Rinsing | Priming a bonding |  | 
Selfetching priming |  |  | Bonding | 
Selfetching bonding) |  |  |  | 
Clinically oriented classification of
the adhesive systems acc
to number of steps

## Slide 35: Srelfetching bonding agents

## Slide 36
TE – Total etch,
ERA
SE – Self etching
SEA

## Slide 37: Two steps selfetching agents
Acidic hydrophilic primer – evaporation of the solvant, penetration, dissolving of the smear layer
Hydrofobic bond – sealing of the surface

## Slide 38: One step selfetching agents
More vulnerable bonding, risk of hydrolysis
FAKT !!!

## Slide 39
Source: Dudek M. Adhezivní spoj
a adhezivní systémy I. LKS 11/2013
Smear layer layer
Dentin
tubules
pH of the adhesive system
thickness of the hybrid layer
surface of dentin smear layer impregnated resin tag
with the adhesive system
very mild acidic sea
mild acidic sea
acidic sea
strong acidic sea

## Slide 40
Colagen fibers with interfibrilar and
Instrafibrilar crystals od hydroxyapatite
Colagen fibers with intrafibrilas crystals
of hydrpoxyapatite only
Colagen fibers without crystals
of hydroxyapatites
Zdroj obrázku: Dudek M. Adhezivní spoj
a adhezivní systémy I. LKS 11/2013

## Slide 41: Importance of hydroxyapatite
Protection of collagen against hydrolysis
as well as enzymatic degradation of collagen (due to activation of matrix metaloproteinasis)
Strong mineral acid id dangereous for good long term bonding
Clorhexidin for one minute can stabilize collagen

## Slide 42
Enzymatic degradation of
collagen

## Slide 44: Factor that influence the quality of bonding
Structure and composition of hard dental tissues
Quality of their surface – esp. presence of smear layer, contamination with moisture, saliva and blood
Configuration factor – C- factor
Mechanical loading of the adhesive connection
Oral environment and external chemical materials (tooth pastes, asntiseptics, bleaching agent rtc.)

## Slide 45: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 46: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 47: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 48
High content of filler increases the modulus of elasticity
High modulus of elasticity increases the polymerization stress
High content of filler decreases the polymerization shrinkage
Polym. Stress
Modulus of elasticity
Polymerization shrinkage

## Slide 49: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 50
5
2
1
Bonded area : Free area
1:1 and less - optimal

## Slide 51: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 52: Mode of application
Incremental technique
Layer by layer with big free surface
Importance of flowables
Thin layer of flowable first –big free surface
Good marginal adaptation
Compensation of the stress of the other layers
Bulk fill materials do not solve the problem with polymerization stress

## Slide 53
Placement of the material

## Slide 54: Polymerization stress depends on
Quality of the material
C- factor
Mode of application
Mode of polymerization

## Slide 55
Monomer
Light
Polymerization
Polymer

## Slide 56
Pre –gel
Gel
Post -gel
Pre gel phase should be long – soft start !!!!

## Slide 57: Three phases
Phases
Pre-gel – material is soft
Gel-point – material became hard
Post –gel – material is not soft, postgel shrinkage

## Slide 58
Fotokompozit
102mm
48mm

## Slide 59
Photocpomosite
3,2mm
57 mm
3mm
8,5mm

## Slide 60
Selfcuring material
434343
43mm
42mm

## Slide 61: Duration of pre-gel phase
Longer pre-gel phase is better for releasing of polymerization stress
Soft start
Combination of materials (selfcuring composite materials have longer pre gel phase)