## Slide 1: C6730 Fázové rovnováhy
P07 Kinetika vzniku vícefázových struktur
Doc. Jiří Sopoušek

## Slide 2: Osnova dnešní přednášky
Termodynamická podmínka vzniku nové fáze
Nukleace
Difúzní a bezdifúzní přeměny
Diskuse
Notes: Dohodnout termín a místo konání přednášky, seznam posluchačů (vč. jejich zaměření)

## Slide 3: Termodynamická podmínka vzniku nové fáze

## Slide 4: Energetika kuloviré částice

## Slide 5: Nukleace nové fáze
Metastabilní stavy: přechlazení a přehřátí

## Slide 6: Možnosti snížení nukleační bariéry

## Slide 7: Metody usnadňující dosažení rovnovážného stavu
Faktory ovlivňující růst nové fáze

## Slide 8: Kinetika fázových transformací
Difúzí řízené bez změny chemického složení a počtu fází (e.g. melting, solidification of pure metal, allotropic transformations, recrystallization, etc.)
Difúzí řízené se změnou chemického složení a počtu fází (e.g. Eutectoid transformations)
Bezdifúzní transformace - produces a metastable phase by cooperative small displacements of all atoms in structure (e.g. martensitic transformation discussed in later in this chapter)

## Slide 9: Kinetika FT
Nucleation of of the new phase - formation of stable small particles (nuclei) of the new phase. Nuclei are often formed at grain boundaries and other defects.
Growth of new phase at the expense of the original phase.

## Slide 10: Rychlost fázové transformace
Rychlost: r = 1 / t0.5
Platí Arrheniova závislost: r = A exp (-QA/kT) = A exp (-Qm/ RT)
Rekrystalizace mědi

## Slide 11: TTT křivky Fe-C
Perlit Fe-0,8wt%C

## Slide 12: Mikrostruktura a TTT křivky
The thickness of the ferrite and cementite layers in pearlite
is ~ 8:1. The absolute layer thickness depends on the
temperature of the transformation. The higher the
temperature, the thicker the layers.

## Slide 13: Bainit
If transformation temperature is low enough (≤540°C)
bainite rather than fine pearlite forms.
Sferitizace (700st)

## Slide 14: Shrnutí difůzně řízených přeměn
The family of S-shaped curves at different T are used to construct the TTT diagrams.
The TTT diagrams are for the isothermal (constant T) transformations (material is cooled quickly to a given temperature before the transformation occurs, and then keep it at that temperature).
At low temperatures, the transformation occurs sooner (it is controlled by the rate of nucleation) and grain growth (that is controlled by diffusion) is reduced.
Slow diffusion at low temperatures leads to fine-grained microstructure with thin-layered structure of pearlite (fine pearlite).
At higher temperatures, high diffusion rates allow for larger grain growth and formation of thick layered structure of pearlite (coarse pearlite). At compositions other than eutectoid, a proeutectoid phase (ferrite or cementite) coexist with pearlite. Additional curves for proeutectoid transformation must be included on TTT diagrams.

## Slide 15: Bezdifúzní přeměny
„Matrenzitické přeměny“

## Slide 16: Martenzit
• Martensite forms when austenite is rapidly quenched to room T.
• The austenite-martensite does not involve diffusion → no thermal activation is needed,this is called an athermal transformation.
• Each atom displaces a small (sub-atomic) distance to transform FCC γ-Fe (austenite) to martensite which has a Body Centered Tetragonal (BCT) unit cell (like BCC, but one unit cell axis is longer than the other two).
• Martensite is metastable - can persist indefinitely at room temperature, but will transform to equilibrium phases on annealing at an elevated temperature. Martensite can coexist with other phases and/or microstructures in Fe-C systém. It does not appear in phase Fe-C phase diagram

## Slide 17: Martenzit
Austenite-to-martensite is diffusionless and very fast. The amount of martensite formed depends on temperature only.

## Slide 18: Tepelné zpracování

## Slide 19: Zpracování Fe-C slitin

## Slide 20: Další fázové transformace

## Slide 21: Tvarová paměť
http://www.youtube.com/watch?v=hMYC-bLMLZQ
http://www.youtube.com/watch?v=fsBHF_j2FJ4
NiTi,

## Slide 22: Diskuse