## Slide 1: Heterogeneous catalysis
Lecture 9
Zeolites in oil refinement

## Slide 2: Zeolites - synthesis
Reaction mixture: …, …, …, …
  pH adjustment, (gelation)
  Hydrothermal treatment in an autoclave
  …
  …
Result: H-zeolite (Brønsted acidic with H+ ions)

## Slide 3: Zeolites - synthesis
Reaction mixture: Na2SiO3, Al2O3, quarternary ammonium salt (=structure directing agent), water
  pH adjustment, (gelation)
  Hydrothermal treatment in an autoclave
  Ion exchange (Na+ for NH4+)
  Calcination (= NH3 removal)
Result: Crystalline H-zeolite (Brønsted acidic with H+ ions)

## Slide 4: Zeolites - synthesis
Pore size
Si/Al ratio ≥ 1
DOI: 10.1039/c3cs60394f

## Slide 5: Zeolites - acidity
Brønsted: …
  Structure:
Lewis: …
  Structure:

## Slide 6: Zeolites - acidity
Brønsted: negative charge of the aluminosilicate net balanced by strongly acidic protons
  Structure:
Lewis: Al atoms that are not embedded in the aluminosilicate net (e.g. surface species, amorphous stuff, alumina particles) = extraframework aluminum species (EFAL)
  Structure:
    H+

## Slide 7: Zeolites - acidity
Brønsted: depends on the second coordination sphere (i.e. Si/Al ratio)
Lewis: Extraframework aluminum species (EFAL) depends on
  Si/Al ratio
  Aging (time on stream, steaming)
  Can be washed out (depending on pH – acid washing)

## Slide 8: Zeolites - acidity
High Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites
Low Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites

## Slide 9: Zeolites - acidity
High Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites
Low Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites

## Slide 10: Zeolites - acidity
Confinement effect
Superacidity
  Various probes at RT – acid site strength similar to 70 % H2SO4 (=NO!)
  Ability to protonate hydrocarbons at working conditions (=YES!)
  ?

## Slide 11: Zeolites – diffusion/shape selectivity
Diffusion
  Big difference between zeolites with 8 membered vs. 12 membered ring pore openings
  Big difference between zeolites with 1D, 2D, and 3D-connected pore structure
Shape selectivity
DOI: 10.1039/c3cs60394f

## Slide 12: Zeolites in oil refinement
Fluid catalytic cracking
Isobutane-butene alkylation
Reforming (+ steam reforming)
Hydrocracking
Linear paraffin isomerization
DOI: 10.1039/c3cs60394f

## Slide 13: Zeolites in oil refinement
Fluid catalytic cracking

## Slide 14: Zeolites in oil refinement
Fluid catalytic cracking
  Zeolite Y 10-50 wt%
  Binders 50-90 wt%
  At the beginning – AlCl3
  Addition of HZSM-5

## Slide 15: Zeolites in oil refinement
Fluid catalytic cracking
  Shortening of long linear hydrocarbons
  Isomerization to branched hydrocarbons
  „Aromatization“
  HZSM-5 for higher propylene production

## Slide 16: Zeolites in oil refinement
Fluid catalytic cracking
  Protonation + protolytic cracking
  H- abstraction + β scission

## Slide 17: Zeolites in oil refinement
Fluid catalytic cracking
  Protonation + protolytic cracking
  H- abstraction + β scission

## Slide 18: Zeolites in oil refinement
Fluid catalytic cracking
  Protonation + protolytic cracking
    We need strong Brøsted acid sites (zeolite Y)
  H- abstraction + β scission
    We need strong Lewis acid sites (steamed/(acid washed) zeolite Y)
  Long linear hydrocarbons diffusion
    Precracking on alumina and silica-alumina (non-innocent binders)
    Hierarchical porosity in zeolites (steamed/(acid washed) zeolite Y)

## Slide 19: Zeolites in oil refinement
Isobutane-butene alkylation
  We want highly branched C8 hydrocarbons (high octane number)
  HF and H2SO4 catalyzed alkylation still running in industry
  Large pore zeolites as a substitution

## Slide 20: Zeolites in oil refinement
Isobutane-butene alkylation
  Large pore zeolites as a substitution
  BUT! 2-butene dimerization…oligomerization…coking…deactivation

## Slide 21: Zeolites in oil refinement
Linear paraffin isomerization
  Linear C8 (C7) → branched C8 (C7)
  Requires strong Brønsted acidity and hydrogenation/dehydrogenation activity (Pt(Ni) on mordenite)
  Mordenite – large pore, monodirectional pores
  Mordenite – dealuminated (strong H+), acid washed (low EFAL)
  Protonation = carbocations
  Stability of carbocations? Branched hydrocarbons?

## Slide 22: Zeolites in oil refinement
Linear paraffin isomerization
  Pt(Ni) on mordenite
  How do we deposit Pt on a zeolite? (Lecture 3)

## Slide 23: Zeolites in oil refinement
Linear paraffin isomerization
  Pt, Pd, Ni on mordenite
  Electrostatic interaction = Ion exchange
    Competitive ion exchange
    [NH4+]

## Slide 24: Zeolites in oil refinement
Linear paraffin isomerization
  Pt, Pd, Ni on mordenite
  Electrostatic interaction = Ion exchange
    Competitive ion exchange

## Slide 25: Zeolites in oil refinement
Hydrocracking (i.e. cracking in the presence of H2)
  Shortening of long hydrocarbons
  From linear to branched (alkylation, carbocations,…)
  Hydrogenation/dehydrogenation
  Pt, Pd on mordenite (also zeolite Y and β)

## Slide 26: Zeolites in oil refinement
Reforming and steam reforming
  Cyclization, isomerization of cyclic compounds to cyclohexene, cyclohexene and its derivatives dehydrogenation to benzene, toluene, xylene (BTX), and other aromatics
  H2 as a useful „by-product“
  Pt on high surface area support, non-acidic
  Reforming in the presence of H2O = H2 production