## Slide 1
Selective Catalytic Reduction
In Automotive
Zdeněk Král

## Slide 2: Selective Catalytic Reduction …in general
Wide technique of NOx removal
  Used everywhere, where NOx is produced (and undesired)
  Used mainly for exhaust gases (chimneys, exhausts, …)
Selective
  We can select which molecule will be reduced (NOx, CO, CO2, SO2)
Catalytic
  Reaction needs to be catalysed.
Reduction
  NOx to N2

## Slide 3: SCR in automotive
Reduction of NOx using reduction agent on a surface of solid catalyst in presence of oxygen
Summary equation: 4NO + 4NH3 + O2 → 4N2 + 6H2O
Other SCR reactions:
  8NH3+ 6NO2 → 7N2 + 12H2O
  … plus many side reactions 2NH3 + NO + NO2 → 2N2 + 3H2O „fast SCR“
Reduction agent
  Needed for high conversion rates
  NH3, HC (hydrocarbons)

## Slide 4: … a bit of History
SCR was developer for industrial applications
  70s - applied in thermal power plants in Japan
  Since 80s – widespread to Europe and USA
First mobile aplications (not powerplants)
  90s Korean cargo ships (diesel engine = electric generator)
  Reason for this application - similar application as in powerplants, steady state of engine operation

## Slide 5: How does SCR catalyst look like?
… of urea
Ceramics carrier with active substance
  SiC, Cordierite
„Mate“
  Heat resisting dense fibers
  Spacer for thermal dilatation
Metal housing
  Stainless steel

## Slide 6: What is the active substance?
… of urea
Several substances are catalytically active enough to be used for SCR
Cu and Fe zeolites (Cu-SSZ-13, Fe-ZSM5)
Metal oxides (V2O5)

## Slide 7: What is the mechanism?
Mechanism is strongly dependent on exact composition of the material

## Slide 8: „State of the Art“
… of urea

## Slide 9: SCR in Automotive
Turbocharger
HOT END
Oxidation cat
DPF+SCR
SCR
ASC
COLD END

## Slide 10: SCR in Automotive
ASC

## Slide 11: NH3-SCR in Automotive
Injection of AdBlue (32,5 % solution of urea in distilled water)
Injection (200°C): H2N-CO-NH2 + H2O → 2NH3 + CO2
1. hydrolysis: H2N-CO-NH2 + H2O → NH3 + HNCO
2. acid w. water: HNCO + H2O → NH3 + CO2