## Slide 1: Heterogeneous catalysis
Lecture 9
Zeolites in oil refinement

## Slide 2: Zeolites - synthesis
Reaction mixture: …, …, …, …
  pH adjustment, (gelation)
  Hydrothermal treatment in an autoclave
  …
  …
Result: H-zeolite (Brønsted acidic with H+ ions)

## Slide 3: Zeolites - synthesis
Reaction mixture: Na2SiO3, Al2O3, quarternary ammonium salt (=structure directing agent), water
  pH adjustment, (gelation)
  Hydrothermal treatment in an autoclave
  Ion exchange (Na+ for NH4+)
  Calcination (= NH3 removal)
Result: Crystalline H-zeolite (Brønsted acidic with H+ ions)

## Slide 4: Zeolites - synthesis
Pore size
Si/Al ratio ≥ 1
DOI: 10.1039/c3cs60394f

## Slide 5: Zeolites - acidity
Brønsted: …
  Structure:
Lewis: …
  Structure:

## Slide 6: Zeolites - acidity
Brønsted: negative charge of the aluminosilicate net balanced by strongly acidic protons
  Structure:
Lewis: Al atoms that are not embedded in the aluminosilicate net (e.g. surface species, amorphous stuff, alumina particles) = extraframework aluminum species (EFAL)
  Structure:
    H+

## Slide 7: Zeolites - acidity
Brønsted: negative charge of the aluminosilicate net balanced by strongly acidic protons
  Structure:
    H+
DOI: 10.1039/C8CS00887F
Changes in local Al structure revealed by EXAFS

## Slide 8: Zeolites - acidity
Brønsted: depends on the second coordination sphere (i.e. Si/Al ratio)
Lewis: Extraframework aluminum species (EFAL) depends on
  Si/Al ratio
  Aging (time on stream, steaming)
  Can be washed out (depending on pH – acid washing)

## Slide 9: Zeolites - acidity
High Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites
Low Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites

## Slide 10: Zeolites - acidity
High Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites
Low Si/Al ratio
  Strong Brønsted acid sites
  Weak Brønsted acid sites
  Strong Lewis acid sites
  Weak Lewis acid sites

## Slide 11: Zeolites - acidity
Confinement effect
Superacidity
  Various probes at RT – acid site strength similar to 70 % H2SO4 (=NO!)
  Ability to protonate hydrocarbons at working conditions (=YES!)
  ?

## Slide 12: Zeolites – diffusion/shape selectivity
Diffusion
  Big difference between zeolites with 8 membered vs. 12 membered ring pore openings
  Big difference between zeolites with 1D, 2D, and 3D-connected pore structure
Shape selectivity
DOI: 10.1039/c3cs60394f

## Slide 13: Other microporous frameworks
Non-Al zeolites
  Be2+, Zn2+, B3+, Ga3+, Fe3+, Ge4+, Ti4+, Sn4+
  15 % variation in radius (vs. Si4+)
  ±0.4 a.u. Pauling electronegativity
Aluminophosphates (AlPOs)
  SiO2 and AlPO4 and isoelectronic structures
  No catalytic activity
M(II) Aluminophosphates
  Mild Brønsted acids and(or) redox catalysts
Silicoaluminophosphates (SAPOs)
  Mild Brønsted acids

## Slide 14: Other microporous frameworks
Non-Al zeolites
  Be2+, Zn2+, B3+, Ga3+, Fe3+, Ge4+, Ti4+, Sn4+
  15 % variation in radius (vs. Si4+)
  ±0.4 a.u. Pauling electronegativity
Lewis acidity in non-Al zeolites
Open vs. Closed acid sites in non-Al zeolites

## Slide 15: Other microporous frameworks
Aluminophosphates (AlPOs)
  M(II) Aluminophosphates
  Silicoaluminophosphates (SAPOs) = milder acidity
DOI: 10.1016/j.cattod.2011.02.027

## Slide 16: Zeolites in oil refinement
Fluid catalytic cracking
Isobutane-butene alkylation
Reforming (+ steam reforming)
Hydrocracking
Linear paraffin isomerization
DOI: 10.1039/c3cs60394f

## Slide 17: Zeolites in oil refinement
Fluid catalytic cracking

## Slide 18: Zeolites in oil refinement
Fluid catalytic cracking
  Zeolite Y 10-50 wt%
  Binders 50-90 wt%
  At the beginning – AlCl3
  Addition of HZSM-5

## Slide 19: Zeolites in oil refinement
Fluid catalytic cracking
  Shortening of long linear hydrocarbons
  Isomerization to branched hydrocarbons
  „Aromatization“
  HZSM-5 for higher propylene production

## Slide 20: Zeolites in oil refinement
Fluid catalytic cracking
  Protonation + protolytic cracking
  H- abstraction + β scission

## Slide 21: Zeolites in oil refinement
Fluid catalytic cracking
  Protonation + protolytic cracking
  H- abstraction + β scission

## Slide 22: Zeolites in oil refinement
Fluid catalytic cracking
  Protonation + protolytic cracking
    We need strong Brøsted acid sites (zeolite Y)
  H- abstraction + β scission
    We need strong Lewis acid sites (steamed/(acid washed) zeolite Y)
  Long linear hydrocarbons diffusion
    Precracking on alumina and silica-alumina (non-innocent binders)
    Hierarchical porosity in zeolites (steamed/(acid washed) zeolite Y)

## Slide 23: Zeolites in oil refinement
Isobutane-butene alkylation
  We want highly branched C8 hydrocarbons (high octane number)
  HF and H2SO4 catalyzed alkylation still running in industry
  Large pore zeolites as a substitution

## Slide 24: Zeolites in oil refinement
Isobutane-butene alkylation
  Large pore zeolites as a substitution
  BUT! 2-butene dimerization…oligomerization…coking…deactivation

## Slide 25: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Linear C8 (C7) → branched C8 (C7)
  Requires strong Brønsted acidity and hydrogenation/dehydrogenation activity (Pt(Ni) on mordenite)
  Mordenite – large pore, monodirectional pores
  Mordenite – dealuminated (strong H+), acid washed (low EFAL)
  Protonation = carbocations
  Stability of carbocations? Branched hydrocarbons?

## Slide 26: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Linear C8 (C7) → branched C8 (C7)
  Requires strong Brønsted acidity and hydrogenation/dehydrogenation activity (Pt(Ni) on mordenite)
  Mechanism???
    Dehydrogenation of n-alkane to n-alkene on Pt
    Diffusion???
    Protonation of n-alkene to secondary carbenium ion on H+ zeolite
    Secondary carbenium ion rearranges to tertiary (more stable) carbenium ion
    Desorption from acid site produces iso-alkene, H+ is restored
    Diffusion???
    Hydrogenation of iso-alkene to iso-alkane on Pt

## Slide 27: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Researchers interested in the effect of “intimacy” (Pt-acid site)
  Affects mainly selectivity, activity to some extent
  An optimum between “too close” and “too far”

## Slide 28: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Researchers interested in the effect of “intimacy” (Pt-acid site)
  Affects mainly selectivity, activity to some extent
  An optimum between “too close” and “too far”
DOI: 10.1021/acscatal.8b01461

## Slide 29: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Pt(Ni) on mordenite
  How do we deposit Pt on a zeolite? (Lecture 3)

## Slide 30: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Pt, Pd, Ni on mordenite
  Electrostatic interaction = Ion exchange
    Competitive ion exchange
    [NH4+]

## Slide 31: Zeolites in oil refinement
Linear paraffin hydroisomerization
  Pt, Pd, Ni on mordenite
  Electrostatic interaction = Ion exchange
    Competitive ion exchange

## Slide 32: Zeolites in oil refinement
Hydrocracking (i.e. cracking in the presence of H2)
  Shortening of long hydrocarbons
  From linear to branched (alkylation, carbocations,…)
  Hydrogenation/dehydrogenation
  Pt, Pd on mordenite (also zeolite Y and β)

## Slide 33: Zeolites in oil refinement
Reforming and steam reforming
  Cyclization, isomerization of cyclic compounds to cyclohexene, cyclohexene and its derivatives dehydrogenation to benzene, toluene, xylene (BTX), and other aromatics
  H2 as a useful „by-product“
  Pt on high surface area support, non-acidic
  Reforming in the presence of H2O = H2 production

## Slide 34: Microporosity of zeolites
+
Regular structure
High stability
Shape selectivity
Confinement effect
−
Diffusion limitations
Coking
Fast deactivation
Solution?
Extra-large pore zeolites
Nanocrystalline zeolites
Hierarchical zeolites
Two-dimensional zeolites
MCM-41, SBA-15 and other mesoporous silica???

## Slide 35: Microporosity of zeolites
+
Regular structure
High stability
Shape selectivity
Confinement effect
−
Diffusion limitations
Coking
Fast deactivation
Solution?
Extra-large pore zeolites
Nanocrystalline zeolites
Hierarchical zeolites
Two-dimensional zeolites
MCM-41, SBA-15 and other mesoporous silica???

## Slide 36: Microporosity of zeolites
Extra-large pore zeolites
  Germanosilicates
  New organic structure-directing agents
  Ge for Al substitution
  Assembly-disassembly-organization-reassembly (prof. Čejka, Prague)
DOI: 10.1039/C8CS00887F

## Slide 37: Microporosity of zeolites
Nanocrystalline zeolites
  Classic hydrothermal synthesis
  But! Part of Si source = MeSi(OEt)3
DOI: 10.1016/j.cattod.2009.04.016

## Slide 38: Microporosity of zeolites
Nanocrystalline zeolites
  Classic hydrothermal synthesis
  But! Part of Si source = MeSi(OEt)3
DOI: 10.1016/j.cattod.2009.04.016
Nano-HZSM-5
Micro-HZSM-5
Ethanol dehydration to ethylene

## Slide 39: Microporosity of zeolites
Hierarchical zeolites
  Add something into the rxn mixture in order to create large pores
    Hard templates (carbon,…)
    Soft templates (alkoxysilanes with a long aliphatic chain)
  Dealumination, desilication
    HNO3, NaOH
DOI: 10.1039/B805502E

## Slide 40: Microporosity of zeolites
Hierarchical zeolites
  Add something into the rxn mixture in order to create large pores
  Dealumination, desilication: alkaline–acid, acid–alkaline, and fluorination–alkaline post-synthesis treatments of H-MOR (below)
DOI: 10.1039/B805502E

## Slide 41: Microporosity of zeolites
Two-dimensional zeolites
  Pillaring
    CTMA+, sonication, surfactant removal = stacked layers
  Delamination
    CTMA+, sonication, TEOS hydrolysis, calcination = layered zeolites with permanently expanded interlayer spaces